EE211 Fall 2025

Homework - Problem Set #6

Due: December 8th, 11:59 pm

Please scan your homework and upload it on the KLMS website.

Problem 1 (10 points)

A Si step junction maintained at room temperature under equilibrium conditions has a p-side doping of NA = 21015 cm-3 and n-side doping of ND = 1015 cm-3. Compute (a) Vbi , (b) xp, xn, and W, (c) E at x = 0, and (d) V at x = 0. (e) Make sketches that are roughly to scale of the charge density, electric field and electrostatic potential as a function of position.

<Solution>

Problem 2 (10 points)

Repeat Problem 1, taking NA = 1017 cm-3 to be the p-side doping. Briefly compare the results here with those of Problem 1.

<Solution>

Problem 3 (10 points)

A pn junction diode has the doping profile sketched as below. Mathematically, ND-NA = N0[1-exp(-αx)], where N0 and α are constants. (a) Give a concise statement of the depletion approximation. (b) Invoking the depletion approximation, make a sketch of the charge density inside the diode. (c) Establish an expression for the electric field E(x), inside the depletion region.

<Solution>

Problem 4 (10 points)

A pn junction diode has the doping profile sketched as below. Assume that xn > x0. (a) What is the built-in potential across the junction? (b) Invoking the depletion approximation, sketch the charge density versus distance inside the diode. (c) Obtain an analytical solution for the electric field, E(x), inside the depletion region.

<Solution>

(a)

(b)

(c)

Problem 5 (10 points)

An “isotype” step junction is one in which the same impurity type doping changes from one concentration value to another value. A p-p isotype doping profile is shown as follows. (a) Sketch the thermal equilibrium energy-band diagram of the isotype junction. (b) Determine the built-in potential barrier. (c) Make rough sketches of the potential, electric field, and charge density inside the junction.

<Solution>

(a)

(b)

For Na =1016 cm-3,

EF-EFi=kTlnNani=0.0259ln10161.5×1010

or

EF-EFi=0.3473 eV

For Na =1015 cm-3,

EF-EFi=0.0259ln10151.5×1010

or

EF-EFi=0.2877 eV

Then,

Vbi=0.34732-0.28768

or

Vbi=0.0596 V

(c)

Problem 6 (10 points)

An abrupt silicon pn junction at T = 300 K has impurity doping concentrations of NA = 51016 cm-3 and ND = 1015 cm-3. Calculate (a) Vbi, (b) W at (i) VR = 0 and (ii) VR = 5 V, and (c) |Emax| at (i) VR = 0 and (ii) VR = 5V.

<Solution>

(a)

Vbi=0.0259ln(5×1016)(1015)(1.5×1010)2=0.6767V

(b)

W= 2∈s(Vbi+VR)eNa+NdNaNd1/2

(i) For VR=0,

W= 2(11.7)(8.85×10-14)(0.6767)1.6×10-19×5×1016+1015(5×1016)(1015)1/2

=9.452×10-5 cm

or

W=0.9452 μm

(ii) For VR=5V,

W= 2(11.7)(8.85×10-14)(0.6767+5)1.6×10-19×5×1016+1015(5×1016)(1015)1/2

=2.738×10-4 cm

or

W=2.738 μm

(c)

Emax=2(Vbi+VR)W

(i) For VR=0,

Emax=2(0.6767)0.9452×10-4=1.43×104 V/cm

(ii) For VR=5V,

Emax=2(0.6767+5)2.738×10-4=4.15×104 V/cm

Problem 7 (10 points)

Consider two p+n silicon junctions at T = 300 K reverse biased at VR = 5 V. The impurity doping concentrations in junction A are NA = 1018 cm-3 and ND = 1015 cm-3, and those in junction B are NA = 1018 cm-3 and ND = 1016 cm-3. Calculate the ratio of the following parameters for junction A to junction B: (a) W, (b) |Emax|, and (c) C’j.

<Solution>

(a)

W(A)W(B)=2∈s(VbiA+VR)eNa+NdANaNdA1/22∈s(VbiB+VR)eNa+NdANaNdB1/2

or

W(A)W(B)=(VbiA+VR)(VbiB+VR)(Na+NdA)(Na+NdB)NdBNdA1/2

We find

VbiA= 0.0259ln(1018)(1015)(1.5×1010)2=0.7543V

VbiB= 0.0259ln(1018)(1016)(1.5×1010)2=0.8139V

We find

W(A)W(B)=5.75435.81391018+10151018+1016×101610151/2

or

W(A)W(B)=3.13

(b)

E(A)E(B)=2(VbiA+VR)W(A)2(VbiB+VR)W(B)=W(B)W(A)∙VbiA+VRVbiB+VR=13.135.75435.8139

or

E(A)E(B)=0.316

(c)

C'j(A)C'j(B)=∈sNaNdA2(VbiA+VR)(Na+NdA)1/2∈sNaNdB2(VbiB+VR)(Na+NdB)1/2=NdANdBVbiB+VRVbiA+VRNa+NdBNa+NdA1/2=101510165.81395.75431018+10161018+10151/2

or

C'j(A)C'j(B)=0.319

Problem 8 (10 points)

Consider a silicon pn junction with the doping profile shown in the figure below. T = 300 K. (a) Calculate the applied reverse-biased voltage (VR) required so that the space charge region extends entirely through the p region. (b) Determine the space charge width into the n+ region with VR calculated in part (a). (c) Calculate the peak electric field for this applied voltage.

<Solution>

An n+p junction with Na = 1014 cm-3,

(a)

A one-sided junction and assume VR >> Vbi.

Then,

xp≅ 2∈sVReNa1/2

or

50×10-42=211.78.85×10-14VR1.6×10-191014

which yields

VR=193 V

(b)

xpxn=NdNa⟹xn=xpNaNd

so

xn=50×10-410141016=0.50×10-4cm=0.50μm

(c)

Emax≅2VRW=2193.1550.5×10-4

or

Emax=7.65×104 V/cm

Problem 9 (10 points)

A diode will very often have the doping profile shown in the figure in Problem 8, which is known as an n+pp+ diode. Under reverse bias, the depletion region must remain within the p-region to avoid premature breakdown. Assume the p-region doping is 1015 cm-3. Determine the reverse-biased voltage such that the depletion region remains within the p region and does not reach breakdown if the p-region width is (a) 75 μm and (b) 150 μm. Refer to the figure below, state whether the maximum depletion width or the breakdown voltage is reached first for each case.

<Solution>

Assume silicon: For an n+p junction

xp= 2∈s(Vbi+VR)eNa1/2

Assume Vbi << VR

(a)

For xp=75μm

(75×10-4)2=2(11.7)(8.85×10-14)VR(1.6×10-19)(1015)

Which yields

VR = 4.35×103 V

(b)

For xp=150μm

(150×10-4)2=2(11.7)(8.85×10-14)VR(1.6×10-19)(1015)

which yields

VR = 1.74×104 V

Note: From Figure 7.15, the breakdown voltage is approximately 300V. So, in each case, breakdown is reached first.

Problem 10 (10 points)

A silicon p-i-n junction has the doping profile shown in the figure below. The ‘i’ corresponds to an ideal intrinsic region in which there is no impurity doping concentration. (a) Draw charge, electric field, and potential briefly. (b) Determine Vbi, xp, xn, and Emax.

<Solution>

(a)

(b)